Description for supplementary videos

Supplementary video S1: Phase separation process is mimicked in this video. A cell filled with the mixture of LC and prepolymer is exposed to a normally incident, collimated UV beam. By adding a suitable photomask during UV exposure process, an additional intensity gradient in the x-y plane of the cell will be then created as well. The NOA65 monomers in the high-intensity regions near the UV beam will firstly undergo polymerization. The NOA65 monomers in the low-intensity regions will diffuse towards the high-intensity regions to maintain their relative concentration and the LCs will be expelled from the polymerization regions inside the cell. With deliberate exposure conditions, long enough UV exposure eventually consumes all the NOA65 monomers and causes LCs to move out of the polymerized volume. Meanwhile, the LC molecules will be also orientated by the alignment layer. Finally, the bilayer structure is formed.

Supplementary video S2: In this video, the sharp focal points were captured by a CCD. When we rotated the polarizer from 0 to 180, the focal points became gradually dim until to fully dark at the polarization angle of 90, then gradually brighter, and finally bright, sharp again.

Supplementary video S3: In this video, when we applied the voltage on the sample, the focal points became dim gradually and finally disappeared.

Supplementary video S4：In this video, we applied the voltage of 9 V on the sample and rotated the polarizer. The image kept dark all the time, indicating that the LC molecules were almost totally realigned along the electric field.

Supplementary video S5：In this video, we moved the position of the LC microlens arrays from the focal plane to the image plane. The image became magnified when we moved the sample to the light source.

Supplementary video S6：In this video, we altered the polarization of the incident light by rotating the polarizer. In the beginning, the polarization of the incident light was parallel to the LC alignment direction. The clear images of the object, a capital letter “F”, were captured by a CCD. When we rotated the polarizer from 0 to 180, the captured image became gradually blurry, and then returned to the clear state again.

Supplementary video S7: In this video, the clear images were captured. When we applied a voltage from 0 to 10 V on the LC microlens arrays, the images became gradually blurry and finally illegible.

Supplementary video S8: In this video, the clear object “3” was captured when the focal plane of the microscopy was on the object “3”. As we continuously moved the microscopy away from the photomask along the optical axis, the object “3” became blurry and the object “D” became clearer gradually.